Technical Data Sheet.

Combikote Primer/Finish

Product Description:	A reinforced modified alkyd with added rust inhibitor formulated for aggressive environments that provides a tough resilient barrier, impermeable to air and moisture, effectively sealing out corrosion. Product has the benefit of being a one coat system (no primer/undercoat necessary). Economical with excellent hiding power, lead free colours, no hazardous solvents, may be overcoated the next day

Uses:	For industrial, agricultural and domestic use. For example, machinery, gates, warehouse doors, steel frames, railings.

Tech.Properties:

Colours:				Restricted range

Finish:			Gloss

Specific Gravity:		0.97

Volume Solids:		40%

Recommended FilmTickness:	75-95micron  WFT/30-40micron DFT

Theoretical Spreading Rate:	10-13m²	/litre

Application Method:		Brush, Roller, Spray

Flash Point:			40˚c

VOC				460g/litre

Drying Times:

10˚C		     20˚C		     30˚C

Touch Dry:		10 hours		6 hours		4 hours

Hard Dry		30 hours		24 hours		18 hours

Min.Overcoat:	24 hours		16 hours		12 hours

Max. Overcoat:	Indefinite	Indefinite	Indefinite

Recommended Systems:		Usually a one coat system

Surface Preparation:	The performance of this coating is directly related to the level of surface preparation. Degrease the substrate to a minimum standard of SSPC-SP1 to remove all oil, grease etc. Power tool clean or wire brush the surface to a minimum standard of ISO 8501:1988 St.2 to remove loose paint, rust etc. All surfaces should be clean and free from atmospheric pollution which may necessitate washing down with fresh, clean water. Allow to dry.

Product Application:	Mixing:			Stir thoroughly before use.

Thinners:		White Spirit

Brush:			Use as supplied

Roller:			Use as supplied

Airless Spray:	Thin with up to 10% White Spirit. Use tip 0.13”-0.17”(0.33mm-0.43mm),  and 2000 – 2400 psi pressure. .

Cleaner: White Spirit

Product Application Cont.

Cleanup Considerations:	All equipment should be cleaned immediately after use with white spirit.

It is advisable that equipment should be cleaned/flushed during the course of application, the frequency of which will depend on the volume of material used and timescale over which applied.

Ensure all waste materials (including packaging) are disposed of in accordance with local regulations.

Health, Safety &

Environmental:	This product must be used in accordance with the Material Data Sheet supplied by Premier Q Coatings Limited.

The user must observe local health, safety and environmental regulations when using this product.

Consult Premier Q Coatings Limited if there are any concerns over the suitability of this product.

Pack Size:	1 litre, 5 litre and 20 litre

Pack Weight:			5 litre:5.2kg

Storage Conditions:		Store away from extremes of temperature.

Limitations:	Do not apply when RH exceeds 88% or the surface is less than 2˚C above dew point. Drying will be affected in cold conditions.

Disclaimer:

The information given in these specifications and technical advice – whether verbal, in writing or by way of trails is for guidance and is given in good faith, but without warranty. This also applies where propriety rights or third parties are involved. Any person using Premier Q Coatings products without first making further enquiries as to the suitability of the products for the intended purpose and testing the products to assess their fitness for the purpose does so at their own risk. The application, use and processing of the products are beyond our control and are therefore your own responsibility, and we can accept no liability for the performance of the products arising out of such use, beyond the value of the goods delivered by us. The information contained in these data sheets is liable to modification from time to time in light of experience and our policy of continuous development.

It is the user’s responsibility to ensure that this sheet is current prior to using the product.