Technical Data Sheet.

Agrikote Farm Oxide

Product Description:	A traditional alkyd based gloss finish for general use, where good covering, gloss and durability are required. Ideal for building and industrial use, on many surfaces.

Uses:	Ideal for general painting and for industrial and agricultural use, where an economical finish is required. Can be used on many surfaces including new and previously painted wood, metal, brick and stone.

Tech.Properties:

Colours:				Red Oxide, Grey Oxide, Green Oxide

Finish:			Full Gloss

Specific Gravity:		0.912

Volume Solids:		47%

Recommended FilmTickness:	80micron  WFT/38micron DFT

Theoretical Spreading Rate:	12m²	/litre

Application Method:		Brush, Roller, Spray

Flash Point:			39˚c

VOC				415g/litre

Drying Times:

10˚C		     20˚C		     30˚C

Touch Dry:		5 hours		3 hours		2 hours

Hard Dry		7 hours		5hours		4hours

Min.Overcoat:	16 hours		12hours		10 hours

Max. Overcoat:	24 hours		24 hours		24 hours

Recommended Systems:		Agrikote ZP Primer Wood Primer

Surface Preparation:	Ensure surfaces are clean, dry and free from dirt, grease and other contamination. Fill holes with suitable filler and prime surfaces with specific primer for the substrate. Sand off old paint work, then wash down with cleaning solution and allow to dry.

Product Application:	Mixing:			Stir thoroughly before use.

Thinners:		White Spirit

Brush:	First coat may be thinned 5% to assist application; two coats should be used for maximum protection and obliteration. Overcoating some strong colours may require an extra to effect full opacity.

Roller:	First coat may be thinned 5% to assist application, two coats should be used for maximum protection and obliteration. . Overcoating some strong colours may require an extra to effect full opacity. A short pile head is recommended when rollering.

Conventional Spray:	Thin with up to 10% White Spirit. Use 50-60 psi pressure and 1.4-1.8mm diameter nozzle.

Airless Spray:	Thin with up to 5% white spirit. Use tip 0.38-0.53mm, 50-60˚ angle and 2000 psi pressure.

Air Assisted Spray: Thin with up to 5% white spirit. Use 8000-1000 psi pressure and 1.4-1.8mm diameter nozzle.

Product Application Cont.	Cleaner: White Spirit

Cleanup Considerations:	All equipment should be cleaned immediately after use with white spirit.

It is advisable that equipment should be cleaned/flushed during the course of application, the frequency of which will depend on the volume of material used and timescale over which applied.

Ensure all waste materials (including packaging) are disposed of in accordance with local regulations.

Health, Safety &

Environmental:	This product must be used in accordance with the Material Data Sheet supplied by Premier Q Coatings Limited.

The user must observe local health, safety and environmental regulations when using this product.

Consult Premier Q Coatings Limited if there are any concerns over the suitability of this product.

Pack Size:	5 and 20litre

Pack Weight:			5 litre:4.56kg 20litre:22.8kg

Storage Conditions:		Store away from extremes of temperature.

Limitations:	Do not apply when RH exceeds 88% or the surface is less than 2˚C above dew point. Drying will be affected in cold conditions.

Disclaimer:

The information given in these specifications and technical advice – whether verbal, in writing or by way of trails is for guidance and is given in good faith, but without warranty. This also applies where propriety rights or third parties are involved. Any person using Premier Q Coatings products without first making further enquiries as to the suitability of the products for the intended purpose and testing the products to assess their fitness for the purpose does so at their own risk. The application, use and processing of the products are beyond our control and are therefore your own responsibility, and we can accept no liability for the performance of the products arising out of such use, beyond the value of the goods delivered by us. The information contained in these data sheets is liable to modification from time to time in light of experience and our policy of continuous development.

It is the user’s responsibility to ensure that this sheet is current prior to using the product.