Technical Data Sheet.

Agrikote ZP Primer

Product Description:	An alkyd based versatile zinc phosphate anticorrosive primer, which gives a high level of protection and adhesion to steelwork. Contains no lead additives and is of low toxicity.

Uses:	Steelwork primer prior to industrial and marine topcoats. Finds use in all environments, agricultural, industrial, and marine. Can be used on non-ferrous metals in conjunction with Etch Primer.

Tech. Properties:

Colours:				White, Light Grey, Mid Grey, Red Oxide

Finish:			Matt

Specific Gravity:		1.30

Volume Solids:			45%

Recommended FilmTickness:	75-150micron WFT / 34 – 68 micron DFT

Theoretical Spreading Rate:	6 – 13m²	/litre

Application Method:		Brush, Roller, Spray

Flash Point:			39˚c

VOC				429 g/litre

Drying Times:

10˚C		     20˚C		     30˚C

Touch Dry:		1 ½ hours	30 minutes	20 minutes

Hard Dry		7 hours		4 hours		3 hours

Min.Overcoat:	10 hours		6 hours		5 hours

Max. Overcoat:	36 hours		24 hours		24 hours

Recommended Systems:

Steel: 	Conventional System: 	Primer: Agrikote ZP Primer

Topcoat:	 Agrikote Machinery Enamel

Extended Life System:	Primer: Agrikote ZP Primer

Intermediate: Standard MIO Primer

Top Coat: Agrikote Machinery Enamel

Aluminium: 			Primer: Etch Primer (2pack)

Intermediate: Agrikote ZP Primer

Top Coat: Agrikote Machinery Enamel

Surface Preparation:	Ensure surfaces are clean, dry and free from dirt, grease and other contamination. Remove scale and rust and prepare to a minimum SA2. Apply two coats of primer in severe environments. On aluminium surfaces apply Etch Primer (2pack) prior to Agrikote ZP Primer for best adhesion.

Product Application:	Mixing:			Stir thoroughly before use.

Thinners:		White Spirit

Brush:			Do not thin. Apply two coats for best results.

Roller:			Do not thin. Apply two coats for best results.

Conventional Spray:	Thin with up to 10% White Spirit. Use 50-60 psi pressure and 1.4-1.8mm diameter nozzle.

Product Application Cont.	Airless Spray:	Thin with up to 5% white spirit. Use tip 0.38-0.53mm, 50-60˚ angle and 2000 psi pressure.

Air Assisted Spray: Thin with up to 5% white spirit. Use 8000-1000 psi pressure and 1.4-1.8mm diameter nozzle.

Cleaner: White Spirit

Cleanup Considerations:	All equipment should be cleaned immediately after use with white spirit.

It is advisable that equipment should be cleaned/flushed during the course of application, the frequency of which will depend on the volume of material used and timescale over which applied.

Ensure all waste materials (including packaging) are disposed of in accordance with local regulations.

Health, Safety &

Environmental:	This product must be used in accordance with the Material Data Sheet supplied by Premier Q Coatings Limited.

The user must observe local health, safety and environmental regulations when using this product.

Consult Premier Q Coatings Limited if there are any concerns over the suitability of this product.

Pack Size:	1 and 5 litre

Pack Weight:			1 litre: 1.3kg	5litre: 6.5kg

Storage Conditions:		Store away from extremes of temperature.

Limitations:	Do not apply when RH exceeds 88% or the surface is less than 2˚C above dew point. Drying will be affected in cold conditions.

Disclaimer:

The information given in these specifications and technical advice – whether verbal, in writing or by way of trails is for guidance and is given in good faith, but without warranty. This also applies where propriety rights or third parties are involved. Any person using Premier Q Coatings products without first making further enquiries as to the suitability of the products for the intended purpose and testing the products to assess their fitness for the purpose does so at their own risk. The application, use and processing of the products are beyond our control and are therefore your own responsibility, and we can accept no liability for the performance of the products arising out of such use, beyond the value of the goods delivered by us. The information contained in these data sheets is liable to modification from time to time in light of experience and our policy of continuous development.

It is the user’s responsibility to ensure that this sheet is current prior to using the product.